9th International Congress of the Serbian Society of Mechanics

July 5-7, 2023, Vrnjačka Banja, Serbia

DESIGNING, OPTIMISING AND FABRICATING OF MICROFLUIDIC DEVICES, BASED ON TOPOLOGY OPTIMISATION AND 3D PRINTING

Dalibor Nikolić1,2, Nevena Milivojević1, Ana Mirić1, Marko Živanović1,2, Nenad Filipović2,3

1Institute for Information Technologies

University of Kragujevac, Jovana Cvijića bb, 34000 Kragujevac, Serbia

e-mail: markovac85@kg.ac.rs, nevena_milivojevic@live.com, anamiric53@gmail.com, zivanovicmkg@gmail.com

2BioIRC - Bioengineering Research and Development Center

University of Kragujevac, Prvoslava Stojanovića 6, 34000 Kragujevac, Serbia

e-mail: markovac85@kg.ac.rs, fica@kg.ac.rs

3Faculty of Engineering

University of Kragujevac, Sestre Janjić 6, 34000 Kragujevac, Serbia

e-mail: fica@kg.ac.rs

Abstract:

Preclinical studies are based on consistent, relevant systems that can be used to better understand basic physiological processes. Flat biology until recently offered us many necessary answers in examining model systems for study of biological processes. However, the reduced use of animal model systems, and limitations of 2D flat biology cell models can be replaced successfully by newer technological in vitro solutions. Flat biology technology is based on static working conditions, in which vasculature and shear forces in most experiments lacks. Also, mimicking of rheological properties of physiological processes are missing. Nowadays, microfluidic chips are one of the most advanced and widely used technologies for in vitro testing of 3D constructs that mimic in vivo processes in a very successful manner. The main challenge in the design of these devices is the consistent distribution of nutrients and drugs. Even the smallest detail in the construction of channels, chambers and other compartments are crucial. This paper presents a unique approach in the design of chip devices by using the computational fluid dynamics (CFD) based on the discretization finite element method (FEM) and topological optimization (TO) method for in silico testing and optimizing the shape of the features (chambers and channels). This approach minimizes mistakes in feature design by minimizing local backflow and recirculation and provides the full potential of novel microfluidic devices.

Key words: microfluidic device, 3D print, topology optimization, Tosca, organ-on-chip

1. Introduction

Biomedical experiments continue to use traditional tissue culture dishes or flasks for cell and tissue cultivation, despite their limitations. These models are generally static and lack vasculature and shear stress forces, typically failing to reproduce the rheological properties of the physiological processes [1]. Similarly, in vivo animal models poorly mimic the human condition and cannot accurately predict drug efficacy, and they are ethically controversial. In this regard, preclinical in vitro experimentation requires highly reliable and physiologically relevant systems that could recapitulate complex human physiology [2]. Over the last two decades, the combination of advanced tissue engineering principles, nanotechnology tools, computer methods and cell biology methods has resulted in the development of a state-of-the-art microfluidic model with an unprecedented ability to reproduce the natural habitat of cells and tissues in microfluidic devices. These biomimetic devices, called organ-on-chip (Organ-on-chip), have become a promising approach that has been applied in numerous research areas. They are beginning to attract the attention of physicians due to their unprecedented predictive capacity and their compatibility with existing technologies, such as optical microscopy, screening techniques or biosensor probes. This provides microfluidic platforms with advanced capabilities that are very attractive for biomedical experimentation, healthcare and the pharmaceutical sector [3, 4].

A wide variety of micro- and bio-fabrication methods have been used to develop these microfluidic devices that contain miniature features (chambers, microchannels). Usually, this type of device is produced by UV photolithography and soft lithography methods, such as replica molding, due to its simplicity and efficiency [5]. In this paper, we are presenting a new approach to fabrication of microfluidic chip devices.

The in vivo environment guarantees the presence of basic molecular factors that direct cell behavior, while vascularization ensures the supply of nutrients and the removal of waste. Therefore, the presence of molecular factors that influence cell division, shape, expansion, proliferation, death and secretion of extracellular matrix components is necessary for successful modeling of morphogenetic events. When designing a 3D model, it should be taken into account that cells in the middle of the construct might behave differently than cells growing on the surface, depending on the nutrient concentration gradient. Specifically, cells respond to dynamic signals, such as electric fields, osmotic and hydrostatic pressure, stress, strain, fluid flow, and flow potential, modifying the surrounding extracellular matrix [6].

The three-dimensional cellular environment plays a synergistic role in directing cell fate and behavior, thus a good replication of the in vivo environment in terms of architecture and mechanical properties is required. The development of a dynamic biomimetic environment is a key aspect in the long-term culture of any cell type or tissue [7, 8]. The main issue with those microfluidic devices is a consistent fluid distribution trues them. The construction of chambers and channels has a huge impact on the distribution of nutrients and drugs in each part of the device (to each testing cells or tissue on a microfluidic chip). This paper also describes a novel approach in designing chip devices by using the computational fluid dynamics (CFD) based on discretization finite element method (FEM) and topological optimization (TO) method for in silico testing and optimizing the shape of the features (chambers and channels). This approach minimizes mistakes in features design by minimizing local backflow and recirculation and provides the full potential of novel microfluidic devices.

2. Material and methods

2.1 Desing of microfluid device

The features of interest, such as chambers and microfluidic channels in form of virtual 3D models, are first designed in the computer-aided design (CAD) software package SolidWorks® Premium 2022 SP0.0 (Fig. 1). The first model was created as a single-chamber chip with one input and one output channel, the simplest lab-on-chip device design (Fig. 1 - right), then, through a series of iterations, that model was updated with the goal of achieving a uniform flow through the chamber.

Fig. 1. SolidWorks® design.

# 2.2 DS SIMULIA® - Tosca fluid topology and non-parametric optimiyation

The Tosca optimization suite provides dedicated fast and powerful flow optimization solutions based on computational fluid dynamics (CFD) simulations. Fluid Optimization enables topology optimization-driven design concepts for fluid flow systems and components. Usually, engineers have to develop innovative products in the shortest development time possible. Tosca has the capability to create innovative design ideas automatically for a defined flow task and optimized flow canals. Fluid Optimization's unique technology helps you achieve the highest flow performance and quality. in the design of the chip, it is very important that, depending on the complexity of the chip, the communication channels must be optimized in such a way that the flow is fully balanced. Also, flow noise must be reduced and flow instabilities are eliminated. In this way, all places inside the chamber/ chambers will be equally covered with the same medium concentration. Zhou et al. [Error: Reference source not found] presented an industrial application of TO for combined conductive and convective heat transfer problems. Flow solution was performed in SIMULIA-Abaqus and optimization process was performed in SIMULIA-Tosca and design dependent convection is modelled. For chip optimization we used 3D model designed by SolidWorks® Premium 2022 SP0.0 software. Ansys® Academic Research Mechanical, Release 19.1 was used for CFD simulations and SIMULIA-Tosca for topology optimization. Topology optimization was performed on inlet canals of the microfluid device (Fig. 2 green area), aim of TO was to create a model with an equal flow in all inlet channels/all camber inputs (Fig. 2 out-A to out-E). Equal flow on all chamber inlets will produce uniform flow thru the chamber.

Fig. 2. CFD Ansys model, boundary conditions

# 2.3 Fabrication of microfluidic chip device

Designed and optimized 3D CAD models was exported to stereolithography (STL) file format. They are precisely delineated to reproduce the desired biological event or microenvironment under study. The STL files were then imported into the 3D printing software. With mask-stereolithography (mSLA) technology, master mold is printed layer by layer.

After 3D printing, replica molding is used to replicate the master. A biocompatible and optically transparent polymeric material, polydimethylsiloxane (PDMS), is used. PDMS elastomer is poured over the mold, and cured in the oven (Fig. 3). The obtained PDMS replica is gently peeled off and cut into appropriate sizes and shapes, and the inlet/outlets are drilled out for tube connection. Finally, controlled UV and ozone radiation is used for bonding the PDMS chip replica to another PDMS part or to a standard microscopy glass slide.

Fig. 3. Cured PDMS chips in mold.

3. Results

The first model was created as a single-chamber chip with one input and one output channel, the simplest lab-on-chip device design (Fig. 1 - right). By using the CFD model simulations the flow true this device was simulated and the results of the velocity field were presented on (Fig. 4). By analyzing the result from the CFD simulation we conclude that the flow true the chamber is unequally distributed and design needs to be updated. Streamlines very well represent the initial state of flow in the microfluidic device as shown in Fig. 4.

Fig. 4. Initial model velocity field – streamlines.

To improve the performance of the device based on intuits our aim was to add several inlet and outlet channels equally distributed on the inlet/outlet chamber plane. By adding several more inlet channels expectation was to create a more uniform flow through the device. The second design was manually updated in CAD software (Fig. 1 - middle) with 5 inputs/outputs channels. The CDF results of fluid flow through that device are presented in (Fig. 53). In this computer model, different inlet canal lengths cause unequal flow and nutrient distribution true cross-section of the chamber. The flow was better than in single canal devices but still have some small distribution irregularity.

Fig. 53. Base model after manual design.

In order to improve the device more and achieve a uniform fluid flow through it, an advanced topological optimization technique was applied. Tosca Fluid - CFD Topology optimization for high-end CFD Software (Fig. 646).

Fig. 64. Optimization process – Tosca Fluid.

Topology optimization process began from 3D model width constant canal width (Fig. 646 up left image). Through a series of iterations and flow simulation using the mass flow balancing algorithm, Tosca changed the geometry of canals by removing discretization elements in according to achieve aimed flow distribution (Fig. 646 up right). In this way TO generate rough design concepts for a desired flow split ratio with multiple given outlets. This design we use as a guide for creating a new smooth CAD model with adequate channel width (Fig. 646 down left image).

The results of CFD velocity distribution in final model after topology optimization are shown in Fig.7. By analyzing the fluid flow streamlines, it can be concluded that this design has achieved uniform fluid flow through the front chamber.

Fig. 7. Final model after optimization.

Channels whose width is not uniform can be very complicated to manufacture, therefore to test the optimized model we printed the master mold for chip replica molding. Fig. 858 shows the fabricated mold (3D printed) before (left) and the final model after optimization (right). Differences in channel width can be easily recognized.

Fig. 85. Fabricated mold channels optimization preview; 
non-optimized inlet canals – left; optimized inlet canals – right

4. Discussion

Compared to conventional microfluidic chip device fabrication techniques, our approach has several advantages. For example, fused deposition-modeling present some restrictions related with the rough surface obtained and the velocity of printing is slow, LCD printing does not have these disadvantages. Also, another technique like Inkjet modeling presents some limitations, including the removal of the support material and the amount of waste produced during the printing process, while there are no such losses with the LCD method. As for stereolithography, there are two main variables along the process, photopolymerizable promoter and resin features. The obtained resolution depends on these two variables, and resolution with this LCD technology is very high [Error: Reference source not found, Error: Reference source not found].

Tosca – topological optimization tool generates models that are difficult to fabricate using conventional fabrication techniques. Therefore, 3D printing is the ideal tool for manufacturing optimized models that can be very complex and, in some cases, can be impossible to manufacture the other way.

5. Conclusions

Using modern computer-aided engineering methods - CFD for in-silico fluid flow analysis, combined with a topological optimization method it is possible to create a chip microfluidic device that will have an equal distribution of fluid flow in all parts, and therefore the examined tissues and cells will have an equal chance of survival. Also, using modern manufacturing technics such as 3D printing that kind of custom-made device is possible to produce and test very easy and very fast.

Considering the biological value of this approach in the creation of microfluidic chip devices, we come to conclusions that can be crucial for the in vitro simulation of in vivo processes. Whatever the dimensions of the chamber in which the 3D culture of the cells being tested is located, the number of cells in most experiments is measured in tens or even hundreds of thousands. If we have a heterogeneous distribution of nutrients and/or drugs in the chip, after a certain time period of the experiment we will get a heterogeneous distribution of (bio)markers that are monitored experimentally. In this sense, the obtained biological results are actually the mean value of biomarker expression in the 3D culture zones that were actually treated differently. Do we really want multiple different treatments within one chip, or we are focused on 1 treatment per 1 chip? On the other hand, using the proposed combination of advanced technologies, we can actually create just that. Namely, if we want, for example, different distribution of drugs, nutrients, oxygen, etc. in different chip compartments, because we mimic a certain physiological process, it is possible.

In any case, to our knowledge, the optimization of microfluidic chip devices in this way has not yet been published. Customized chip design will be imperative in many in vivo like experiments on chip devices in the future, and this work will certainly contribute to a better understanding of the topic being addressed.

Acknowledgments

This work was supported by Ministry of Education, Science and Technological Development of the Republic of Serbia (Agreement no. 451-03-68/2022-14/200107). Also, we owe special thanks to Dr. J Miguel Oliveira (3BS Research Group, University of Minho, Portugal) for introducing our research group to the scientific field of using PDMS in the production of microfluidic chip devices. This work is supported by the European Union’s Horizon 2020 research and innovation pro-gramme under grant agreement No 952603 (SGABU). This article reflects only the author's view. The Commission is not responsible for any use that may be made of the information it contains.

References

- Carvalho MR, Barata D, Teixeira LM, Giselbrecht S, Reis RL, Oliveira JM, Truckenmüller R, Habibovic P. Colorectal tumor-on-a-chip system: A 3D tool for precision onco-nanomedicine.Sci Adv. 2019 May 22;5(5): eaaw1317. doi: 10.1126/sciadv. aaw1317.

- Zhang YS, Aleman J, Shin SR, Kilic T, Kim D, Mousavi Shaegh SA, Massa S, Riahi R, Chae S, Hu N, Avci H, Zhang W, Silvestri A, Sanati Nezhad A, Manbohi A, De Ferrari F, Polini A, Calzone G, Shaikh N, Alerasool P, Budina E, Kang J, Bhise N, Ribas J, Pourmand A, Skardal A, Shupe T, Bishop CE, Dokmeci MR, Atala A, Khademhosseini A. Multisensor-integrated organs-on-chips platform for automated and continual in situ monitoring of organoid behaviors. Proc Natl Acad Sci U S A. 2017 Mar 21;114(12): E2293-E2302. doi: 10.1073/pnas.1612906114.

- David Caballero, Maria AngélicaLuque-González, Rui L. Reis, Subhas C. Kundu, Chapter 15 - Microfluidic systems in cancer research, Biomaterials for 3D Tumor Modeling, Elsevier, 2020, Pages 331-377, ISBN 9780128181287, doi: 10.1016/B978-0-12-818128-7.00015-0.

- Bower R, Green VL, Kuvshinova E, Kuvshinov D, Karsai L, Crank ST, Stafford ND, Greenman J. Maintenance of head and neck tumor on-chip: gateway to personalized treatment? Future Sci OA. 2017 Mar 7;3(2): FSO174. doi: 10.4155/fsoa-2016-0089.

- Carvalho, M.R., Carvalho, C.R., Maia, F.R., Caballero, D., Kundu, S.C., Reis, R.L. and Oliveira, J.M. (2019), Peptide-Modified Dendrimer Nanoparticles for Targeted Therapy of Colorectal Cancer. Adv. Therap., 2: 1900132. doi: 10.1002/adtp.201900132.

- Raimondi MT. Engineered tissue as a model to study cell and tissue function from a biophysical perspective. Curr. Drug Discov. Technol. 2006. 3, 245–268. doi: 10.2174/157016306780368126.

- Baker M. Tissue models: a living system on a chip. Nature. 2011. 471, 661–665. doi:10.1038/471661a.

- Esch EW, Bahinski A, Huh D. Organs-on-chips at the frontiers of drug discovery. Nat. Rev. Drug Discov. 2015. 14, 248–260. doi: 10.1038/nrd4539.

- Zhou, M., Alexandersen, J., Sigmund, O. et al. Industrial application of topology optimization for combined conductive and convective heat transfer problems. Struct Multidisc Optim 54, 1045–1060 (2016). https://doi.org/10.1007/s00158-016-1433-2

- Waheed S, Cabot JM, Macdonald NP, Lewis T, Guijt RM, Paull B, Breadmore MC. 3D printed microfluidic devices: enablers and barriers. Lab Chip. 2016 May 24; 16(11): 1993-2013. doi: 10.1039/c6lc00284f.

- Macdonald NP, Cabot JM, Smejkal P, Guijt RM, Paull B, Breadmore MC. Comparing Microfluidic Performance of Three-Dimensional (3D) Printing Platforms. Anal Chem. 2017 Apr 4; 89(7): 3858-3866. doi: 10.1021/acs.analchem.7b00136.